AMALIE XLO Ultimate Full Synthetic Molybdenum Fortified CK-4/SN

5W-40

(September 2017 edition)

AMALIE XLO Full Synthetic Molybdenum Fortified CK-4/SN 5W-40 is full synthetic high-performance diesel engine oil utilizing the latest in additive technology to offer the ultimate protection of your engine.  Designed to meet or exceed the latest OEM and API CK-4 requirements, it is also backwards compatible to previous OEM and API specifications such as CJ-4, CI-4, CI-4+, and CH-4.  Amalie CK-4/SN 5W-40 carries the API SN classification for use in gasoline engines and is an excellent choice for operators with mixed fleets.  This oil is specially designed to protect EGR/Low-Emission Diesel Engines while maximizing the durability of Diesel Particulate Filters (DPF’s).

AMALIE XLO Full Synthetic Molybdenum Fortified CK-4/SN 5W-40 is recommended for use in a wide range of heavy-duty applications and operating environments found on-and off-highway, including engines operating under heavy loads. It is formulated for extended service/extended drain when operated under typical operating conditions. Amalie CK-4/SN 5W-40 offers improved TBN retention, lower oil consumption, greater wear protection, oxidation stability, excellent shear stability, and reduced high temperature deposits.

Benefits:

- High soot handling

- Improved sludge control

- Excellent protection for metal components from rust, corrosion and wear

- Superior oxidation stability

- Shear stable formulation

- One oil for mixed Fleets

- Exceptional oil consumption control

- Lasting TBN retention

- Excellent Low Temperature Pumpability

Typical Physical and Chemical Properties

Viscosity Grade…………………………………………………………………………………......5W-40

Kinematic Viscosity @100°C, cSt………………………………………………………….……..14.40

Kinematic Viscosity @40°C, cSt………………………………………………………………….88.70

Viscosity Index…………………………………………………………………………………..….170

Flash Point, °C (°F)………………………………………………………………………….……..220(428)

Pour Point, °C (°F)……………………………………………………………………….………...-42(-43.6)

Density, S.G….…………………………………………………………………………..………….0.861

Sulfated Ash, Wt%.................................................................................................................1.0

TBN, mgKOH/g……………………………………………………………………………………..11.0

Typical values are listed.  Variations not affecting the performance of this fluid may occur during production however; these variations will not fall outside of set specification parameters.

AMALIE XLO Ultimate Full Synthetic Molybdenum Fortified CK-4/SN

5W-40

Approvals and Recommendations

| SPECIFICATIONS | Amalie 5W-40 |
| --- | --- |
| ACEA: |  |
| E9, E7 | √ |
| API: |  |
| CK-4, CJ-4, CI-4 PLUS, CI-4, CH-4 | √ |
| SN, SM, SL, SJ | √ |
| Caterpillar |  |
| ECF-3, ECF-2 | √ |
| Chrysler |  |
| MS-10902 | √ |
| Cummins: |  |
| CES 20086, CES 20081 | √ |
| Daimler (MB) |  |
| MB 228.31 | √ |
| Detroit Diesel |  |
| DFS 93K222, 93K218 | √ |
| Deutz |  |
| DQC III-10 LA | √ |
| Ford |  |
| WSS M2C171-F1 | √ |
| Global |  |
| DHD-1 | √ |
| JASO |  |
| DH-2, DH-1 | √ |
| Mack |  |
| EOS-4.5, EO-O Premium Plus, EO-N | √ |
| MAN |  |
| M 3575 | √ |
| Mil-PRF |  |
| 2104 Rev. H | √ |
| MTU |  |
| 2.1 | √ |
| Navistar |  |
| TSI-99-12 | √ |
| Renault |  |
| RLD-4, RLD-3 | √ |
| Volvo |  |
| VDS-4.5, VDS-4, VDS 3 | √ |

Please consult Amalie Technical Services or your local representative for a full listing of applications.